(1)

Table 1. Temperature, wire diameter, weight and stress for each test.

| run | Temp (celsius) | Temp(Kelvin) | Load (Lb) | Stress (Psi) | average diameter (inches) |
| --- | --- | --- | --- | --- | --- |
| 1 | 925 | 1198 | 3.30141845 | 15636.63221 | 0.0164 |
| 2 | 950 | 1223 | 3.30141845 | 15636.63221 | 0.0164 |
| 3 | 975 | 1248 | 3.30141845 | 15636.63221 | 0.0164 |
| 4 | 975 | 1248 | 2.86159676 | 13553.48822 | 0.0164 |
| 5 | 975 | 1248 | 2.64444169 | 12524.9685 | 0.0164 |

(2A)

Table 2A. Run 1

| Time (seconds | Elongation ( inch) | strain |
| --- | --- | --- |
| 0 | 0 | 0 |
| 10 | 0.06 | 0.010118044 |
| 20 | 0.07 | 0.011804384 |
| 30 | 0.13 | 0.021922428 |
| 40 | 0.19 | 0.032040472 |
| 50 | 0.21 | 0.035413153 |
| 60 | 0.23 | 0.038785835 |
| 70 | 0.25 | 0.042158516 |
| 80 | 0.26 | 0.043844857 |
| 90 | 0.26 | 0.043844857 |
| 100 | 0.3 | 0.050590219 |
| 110 | 0.33 | 0.055649241 |
| 120 | 0.35 | 0.059021922 |
| 130 | 0.35 | 0.059021922 |
| 140 | 0.43 | 0.072512648 |
| 150 | 0.44 | 0.074198988 |
| 160 | 0.38 | 0.064080944 |
| 170 | 0.39 | 0.065767285 |
| 180 | 0.4 | 0.067453626 |
| 190 | 0.4 | 0.067453626 |
| 200 | 0.41 | 0.069139966 |
| 210 | 0.56 | 0.094435076 |
| 220 | 0.61 | 0.102866779 |
| 230 | 0.62 | 0.10455312 |
| 240 | 0.64 | 0.107925801 |
| 250 | 0.64 | 0.107925801 |
| 260 | 0.65 | 0.109612142 |
| 270 | 0.66 | 0.111298482 |
| 280 | 0.71 | 0.119730185 |
| 290 | 0.72 | 0.121416526 |
| 300 | 0.75 | 0.126475548 |
| 310 | 0.79 | 0.133220911 |
| 320 | 0.9 | 0.151770658 |
| 330 | 0.96 | 0.161888702 |
| 340 | 1.02 | 0.172006745 |
| 350 | 1.02 | 0.172006745 |
| 360 | 1.06 | 0.178752108 |
| 370 | 1.2 | 0.202360877 |
| 380 | 1.2 | 0.202360877 |
| 390 | 1.24 | 0.209106239 |
| 400 | 1.25 | 0.21079258 |
| 410 | 1.28 | 0.215851602 |
| 420 | 1.29 | 0.217537943 |
| 430 | 1.3 | 0.219224283 |
| 440 | 1.31 | 0.220910624 |
| 450 | 1.4 | 0.23608769 |
| 460 | 1.44 | 0.242833052 |
| 470 | 1.48 | 0.249578415 |
| 480 | 1.53 | 0.258010118 |
| 490 | 1.59 | 0.268128162 |
| 500 | 1.66 | 0.279932546 |
| 510 | 1.69 | 0.284991568 |
| 520 | 1.7 | 0.286677909 |
| 530 | 1.75 | 0.295109612 |
| 540 | 1.77 | 0.298482293 |
| 550 | 1.8 | 0.303541315 |
| 560 | 1.8 | 0.303541315 |
| 570 | 1.8 | 0.303541315 |
| 580 | 1.85 | 0.311973019 |
| 590 | 1.9 | 0.320404722 |
| 600 | 2.01 | 0.338954469 |
| 610 | 2.04 | 0.344013491 |
| 620 | 2.06 | 0.347386172 |
| 630 | 2.06 | 0.347386172 |
| 640 | 2.1 | 0.354131535 |
| 650 | 2.21 | 0.372681282 |
| 660 | 2.3 | 0.387858347 |
| 670 | 2.3 | 0.387858347 |
| 680 | 2.3 | 0.387858347 |
| 690 | 2.34 | 0.39460371 |
| 700 | 2.37 | 0.399662732 |
| 710 | 2.44 | 0.411467116 |
| 720 | 2.53 | 0.426644182 |
| 730 | 2.56 | 0.431703204 |
| 740 | 2.6 | 0.438448567 |
| 750 | 2.67 | 0.450252951 |
| 760 | 2.71 | 0.456998314 |
| 770 | 2.76 | 0.465430017 |
| 780 | 2.8 | 0.472175379 |
| 790 | 2.84 | 0.478920742 |
| 800 | 2.87 | 0.483979764 |
| 810 | 2.93 | 0.494097808 |
| 820 | 2.96 | 0.49915683 |
| 830 | 3 | 0.505902192 |
| 840 | 3.04 | 0.512647555 |
| 850 | 3.07 | 0.517706577 |
| 860 | 3.2 | 0.539629005 |
| 870 | 3.24 | 0.546374368 |
| 880 | 3.26 | 0.549747049 |
| 890 | 3.36 | 0.566610455 |
| 900 | 3.4 | 0.573355818 |
| 910 | 3.5 | 0.590219224 |
| 920 | 3.58 | 0.603709949 |
| 930 | 3.61 | 0.608768971 |
| 940 | 3.73 | 0.629005059 |
| 950 | 3.76 | 0.634064081 |
| 960 | 3.8 | 0.640809444 |
| 970 | 3.89 | 0.655986509 |
| 980 | 4 | 0.674536256 |
| 990 | 4.09 | 0.689713322 |
| 1000 | 4.17 | 0.703204047 |
| 1010 | 4.3 | 0.725126476 |
| 1020 | 4.53 | 0.76391231 |

Table 2B. Run 2

| Time (seconds | Elongation ( inch) | strain |
| --- | --- | --- |
| 0 | 0 | 0 |
| 10 | 0.05 | 0.008431703 |
| 20 | 0.09 | 0.015177066 |
| 30 | 0.13 | 0.021922428 |
| 40 | 0.19 | 0.032040472 |
| 50 | 0.26 | 0.043844857 |
| 60 | 0.36 | 0.060708263 |
| 70 | 0.52 | 0.087689713 |
| 80 | 0.52 | 0.087689713 |
| 90 | 0.6 | 0.101180438 |
| 100 | 0.65 | 0.109612142 |
| 110 | 0.71 | 0.119730185 |
| 120 | 0.85 | 0.143338954 |
| 130 | 0.86 | 0.145025295 |
| 140 | 0.94 | 0.15851602 |
| 150 | 1.06 | 0.178752108 |
| 160 | 1.06 | 0.178752108 |
| 170 | 1.16 | 0.195615514 |
| 180 | 1.11 | 0.187183811 |
| 190 | 1.23 | 0.207419899 |
| 200 | 1.27 | 0.214165261 |
| 210 | 1.29 | 0.217537943 |
| 220 | 1.34 | 0.225969646 |
| 230 | 1.52 | 0.256323777 |
| 240 | 1.59 | 0.268128162 |
| 250 | 1.63 | 0.274873524 |
| 260 | 1.71 | 0.28836425 |
| 270 | 1.78 | 0.300168634 |
| 280 | 1.9 | 0.320404722 |
| 290 | 1.91 | 0.322091062 |
| 300 | 1.92 | 0.323777403 |
| 310 | 2 | 0.337268128 |
| 320 | 2.08 | 0.350758853 |
| 330 | 2.2 | 0.370994941 |
| 340 | 2.29 | 0.386172007 |
| 350 | 2.3 | 0.387858347 |
| 360 | 2.43 | 0.409780776 |
| 370 | 2.5 | 0.42158516 |
| 380 | 2.59 | 0.436762226 |
| 390 | 2.69 | 0.453625632 |
| 400 | 2.76 | 0.465430017 |
| 410 | 2.82 | 0.475548061 |
| 420 | 2.84 | 0.478920742 |
| 430 | 2.92 | 0.492411467 |
| 440 | 3.04 | 0.512647555 |
| 450 | 3.18 | 0.536256324 |
| 460 | 3.23 | 0.544688027 |
| 470 | 3.34 | 0.563237774 |
| 480 | 3.47 | 0.585160202 |
| 490 | 3.61 | 0.608768971 |
| 500 | 3.7 | 0.623946037 |
| 510 | 3.78 | 0.637436762 |
| 520 | 3.85 | 0.649241147 |
| 530 | 3.99 | 0.672849916 |
| 540 | 4.15 | 0.699831366 |
| 550 | 4.33 | 0.730185497 |
| 560 | 4.49 | 0.757166948 |
| 570 | 4.66 | 0.785834739 |
| 580 | 4.82 | 0.812816189 |
| 590 | 5.1 | 0.860033727 |

Table 2C. Run 3

| Time (seconds | elongation | strain |
| --- | --- | --- |
| 0 | 0 | 0 |
| 5 | 0.03 | 0.005059022 |
| 10 | 0.13 | 0.021922428 |
| 15 | 0.15 | 0.02529511 |
| 20 | 0.15 | 0.02529511 |
| 25 | 0.15 | 0.02529511 |
| 30 | 0.17 | 0.028667791 |
| 35 | 0.21 | 0.035413153 |
| 40 | 0.32 | 0.053962901 |
| 45 | 0.36 | 0.060708263 |
| 50 | 0.36 | 0.060708263 |
| 55 | 0.43 | 0.072512648 |
| 60 | 0.44 | 0.074198988 |
| 65 | 0.52 | 0.087689713 |
| 70 | 0.52 | 0.087689713 |
| 75 | 0.6 | 0.101180438 |
| 80 | 0.66 | 0.111298482 |
| 85 | 0.7 | 0.118043845 |
| 90 | 0.72 | 0.121416526 |
| 95 | 0.76 | 0.128161889 |
| 100 | 0.84 | 0.141652614 |
| 105 | 0.84 | 0.141652614 |
| 110 | 0.9 | 0.151770658 |
| 115 | 0.96 | 0.161888702 |
| 120 | 0.99 | 0.166947723 |
| 125 | 1.13 | 0.190556492 |
| 130 | 1.15 | 0.193929174 |
| 135 | 1.2 | 0.202360877 |
| 140 | 1.27 | 0.214165261 |
| 145 | 1.27 | 0.214165261 |
| 150 | 1.33 | 0.224283305 |
| 155 | 1.37 | 0.231028668 |
| 160 | 1.44 | 0.242833052 |
| 165 | 1.49 | 0.251264755 |
| 170 | 1.56 | 0.26306914 |
| 175 | 1.61 | 0.271500843 |
| 180 | 1.61 | 0.271500843 |
| 185 | 1.62 | 0.273187184 |
| 190 | 1.69 | 0.284991568 |
| 195 | 1.82 | 0.306913997 |
| 200 | 1.83 | 0.308600337 |
| 205 | 1.89 | 0.318718381 |
| 210 | 1.9 | 0.320404722 |
| 215 | 1.93 | 0.325463744 |
| 220 | 2.01 | 0.338954469 |
| 225 | 2.03 | 0.34232715 |
| 230 | 2.15 | 0.362563238 |
| 235 | 2.28 | 0.384485666 |
| 240 | 2.33 | 0.392917369 |
| 245 | 2.36 | 0.397976391 |
| 250 | 2.41 | 0.406408094 |
| 255 | 2.53 | 0.426644182 |
| 260 | 2.63 | 0.443507589 |
| 265 | 2.73 | 0.460370995 |
| 270 | 2.83 | 0.477234401 |
| 275 | 2.88 | 0.485666105 |
| 280 | 2.89 | 0.487352445 |
| 285 | 2.97 | 0.50084317 |
| 290 | 3.06 | 0.516020236 |
| 295 | 3.15 | 0.531197302 |
| 300 | 3.29 | 0.554806071 |
| 305 | 3.37 | 0.568296796 |
| 310 | 3.49 | 0.588532884 |
| 315 | 3.59 | 0.60539629 |
| 320 | 3.71 | 0.625632378 |
| 325 | 3.83 | 0.645868465 |
| 330 | 3.97 | 0.669477234 |
| 335 | 3.23 | 0.544688027 |

Table 2D. Run 4

| time | elongation | strain |
| --- | --- | --- |
| 0 | 0 | 0 |
| 5 | 0.05 | 0.008431703 |
| 10 | 0.1 | 0.016863406 |
| 15 | 0.12 | 0.020236088 |
| 20 | 0.13 | 0.021922428 |
| 25 | 0.15 | 0.02529511 |
| 30 | 0.22 | 0.037099494 |
| 35 | 0.35 | 0.059021922 |
| 40 | 0.36 | 0.060708263 |
| 45 | 0.4 | 0.067453626 |
| 50 | 0.46 | 0.077571669 |
| 55 | 0.49 | 0.082630691 |
| 60 | 0.52 | 0.087689713 |
| 65 | 0.59 | 0.099494098 |
| 70 | 0.69 | 0.116357504 |
| 75 | 0.71 | 0.119730185 |
| 80 | 0.75 | 0.126475548 |
| 85 | 0.78 | 0.13153457 |
| 90 | 0.81 | 0.136593592 |
| 95 | 0.89 | 0.150084317 |
| 100 | 0.89 | 0.150084317 |
| 105 | 0.91 | 0.153456998 |
| 110 | 0.97 | 0.163575042 |
| 115 | 1.08 | 0.182124789 |
| 120 | 1.08 | 0.182124789 |
| 125 | 1.14 | 0.192242833 |
| 130 | 1.18 | 0.198988196 |
| 135 | 1.2 | 0.202360877 |
| 140 | 1.26 | 0.212478921 |
| 145 | 1.31 | 0.220910624 |
| 150 | 1.35 | 0.227655987 |
| 155 | 1.39 | 0.234401349 |
| 160 | 1.46 | 0.246205734 |
| 165 | 1.51 | 0.254637437 |
| 170 | 1.55 | 0.261382799 |
| 175 | 1.6 | 0.269814503 |
| 180 | 1.66 | 0.279932546 |
| 185 | 1.7 | 0.286677909 |
| 190 | 1.75 | 0.295109612 |
| 195 | 1.81 | 0.305227656 |
| 200 | 1.88 | 0.31703204 |
| 205 | 1.91 | 0.322091062 |
| 210 | 1.95 | 0.328836425 |
| 215 | 2.08 | 0.350758853 |
| 220 | 2.2 | 0.370994941 |
| 225 | 2.2 | 0.370994941 |
| 230 | 2.22 | 0.374367622 |
| 235 | 2.39 | 0.403035413 |
| 240 | 2.44 | 0.411467116 |
| 245 | 2.48 | 0.418212479 |
| 250 | 2.51 | 0.423271501 |
| 255 | 2.6 | 0.438448567 |
| 260 | 2.61 | 0.440134907 |
| 265 | 2.71 | 0.456998314 |
| 270 | 2.85 | 0.480607083 |
| 275 | 2.9 | 0.489038786 |
| 280 | 2.97 | 0.50084317 |
| 285 | 3.06 | 0.516020236 |
| 290 | 3.2 | 0.539629005 |
| 295 | 3.27 | 0.55143339 |
| 300 | 3.35 | 0.564924115 |
| 305 | 3.46 | 0.583473862 |
| 310 | 3.64 | 0.613827993 |
| 315 | 3.77 | 0.635750422 |
| 320 | 3.9 | 0.65767285 |
| 325 | 3.95 | 0.666104553 |
| 330 | 4.29 | 0.723440135 |

Table 2E. Run 5

| Time | elongation (inch) | strain |
| --- | --- | --- |
| 0 | 0 | 0 |
| 5 | 0.02 | 0.003372681 |
| 10 | 0.04 | 0.006745363 |
| 15 | 0.05 | 0.008431703 |
| 20 | 0.07 | 0.011804384 |
| 25 | 0.09 | 0.015177066 |
| 30 | 0.1 | 0.016863406 |
| 35 | 0.17 | 0.028667791 |
| 40 | 0.22 | 0.037099494 |
| 45 | 0.26 | 0.043844857 |
| 50 | 0.3 | 0.050590219 |
| 55 | 0.37 | 0.062394604 |
| 60 | 0.42 | 0.070826307 |
| 65 | 0.47 | 0.07925801 |
| 70 | 0.49 | 0.082630691 |
| 75 | 0.51 | 0.086003373 |
| 80 | 0.57 | 0.096121417 |
| 85 | 0.58 | 0.097807757 |
| 90 | 0.58 | 0.097807757 |
| 95 | 0.58 | 0.097807757 |
| 100 | 0.59 | 0.099494098 |
| 105 | 0.66 | 0.111298482 |
| 110 | 0.72 | 0.121416526 |
| 115 | 0.78 | 0.13153457 |
| 120 | 0.8 | 0.134907251 |
| 125 | 0.81 | 0.136593592 |
| 130 | 0.81 | 0.136593592 |
| 135 | 0.83 | 0.139966273 |
| 140 | 0.85 | 0.143338954 |
| 145 | 0.97 | 0.163575042 |
| 150 | 1 | 0.168634064 |
| 155 | 1 | 0.168634064 |
| 160 | 1.06 | 0.178752108 |
| 165 | 1.11 | 0.187183811 |
| 170 | 1.11 | 0.187183811 |
| 175 | 1.11 | 0.187183811 |
| 180 | 1.13 | 0.190556492 |
| 185 | 1.19 | 0.200674536 |
| 190 | 1.24 | 0.209106239 |
| 195 | 1.33 | 0.224283305 |
| 200 | 1.37 | 0.231028668 |
| 205 | 1.47 | 0.247892074 |
| 210 | 1.52 | 0.256323777 |
| 215 | 1.54 | 0.259696459 |
| 220 | 1.54 | 0.259696459 |
| 225 | 1.54 | 0.259696459 |
| 230 | 1.61 | 0.271500843 |
| 235 | 1.7 | 0.286677909 |
| 240 | 1.74 | 0.293423272 |
| 245 | 1.8 | 0.303541315 |
| 250 | 1.8 | 0.303541315 |
| 255 | 1.83 | 0.308600337 |
| 260 | 1.86 | 0.313659359 |
| 265 | 1.88 | 0.31703204 |
| 270 | 1.95 | 0.328836425 |
| 275 | 2 | 0.337268128 |
| 280 | 2 | 0.337268128 |
| 285 | 2.04 | 0.344013491 |
| 290 | 2.08 | 0.350758853 |
| 295 | 2.11 | 0.355817875 |
| 300 | 2.17 | 0.365935919 |
| 305 | 2.25 | 0.379426644 |
| 310 | 2.28 | 0.384485666 |
| 315 | 2.32 | 0.391231029 |
| 320 | 2.37 | 0.399662732 |
| 325 | 2.43 | 0.409780776 |
| 330 | 2.5 | 0.42158516 |
| 335 | 2.54 | 0.428330523 |
| 340 | 2.58 | 0.435075885 |
| 345 | 2.6 | 0.438448567 |
| 350 | 2.65 | 0.44688027 |
| 355 | 2.65 | 0.44688027 |
| 360 | 2.7 | 0.455311973 |
| 365 | 2.8 | 0.472175379 |
| 370 | 2.85 | 0.480607083 |
| 375 | 2.86 | 0.482293423 |
| 380 | 2.9 | 0.489038786 |
| 385 | 2.93 | 0.494097808 |
| 390 | 3.01 | 0.507588533 |
| 395 | 3.08 | 0.519392917 |
| 400 | 3.14 | 0.529510961 |
| 405 | 3.16 | 0.532883642 |
| 410 | 3.28 | 0.55311973 |
| 415 | 3.38 | 0.569983137 |
| 420 | 3.47 | 0.585160202 |
| 425 | 3.54 | 0.596964587 |
| 430 | 3.61 | 0.608768971 |
| 435 | 3.69 | 0.622259696 |
| 440 | 3.79 | 0.639123103 |
| 445 | 3.9 | 0.65767285 |
| 450 | 3.99 | 0.672849916 |
| 455 | 4.04 | 0.681281619 |
| 460 | 4.13 | 0.696458685 |
| 465 | 4.26 | 0.718381113 |
| 470 | 4.5 | 0.758853288 |

(2B)

Figure 1.Creep Curve for Run 1

Figure 2. Creep Curve for Run 2

Figure 3 Creep Curve for Run 3

Figure 4. Creep Curve for Run 4

Figure 5. Creep Curve for Run 5

(2C)

Figure 6. Creep Curve for Run 1

Figure 7. Creep Curve for Run 2

Figure 8. Creep Curve for Run 3

Figure 9. Creep Curve for Run 4

Figure 10. Creep Curve for Run 5

The minimum creep rate, εmin or εSS, is found by taking the minimum slope of the best fit curve, and drawing a line tangent to the curve at this point. The slope of this linear equation is then the minimum creep rate.

(2D)

Table 3. Stress, temperature, minimum creep rate, and time to fracture for experiments 1 to 5

| run | Temp (celsius) | Temp(Kelvin) | Stress (Psi) | Steady-State Creep Rate (min.-1) | Time to Fracture (minutes) |
| --- | --- | --- | --- | --- | --- |
| 1 | 925 | 1198 | 15636.63221 | 0.039 | 17 |
| 2 | 950 | 1223 | 15636.63221 | 0.0812 | 9.83 |
| 3 | 975 | 1248 | 15636.63221 | 0.0983 | 5.5 |
| 4 | 975 | 1248 | 13553.48822 | 0.1041 | 5.5 |
| 5 | 975 | 1248 | 12524.9685 | 0.0698 | 7.83 |

(3A)

εSS=Ce-QRT

εSSC=e-QRT

lnεSSC=-QRT

lnεSS-lnC=-QRT

lnεSS=-QRT+lnC

lnεSS=-QR1T+lnC

For the form, y=mx+b, y=lnεSS, k=-QR, x=1T, and m=lnC.

(3B)

Figure 11. Plot of natural log of steady state creep rate vs. 1/temperature

(3C)

Figure 12 Plot of natural log of steady state creep rate vs. 1/temperature

From Figure 12, the equation of the straight line thorough the data is

y= -27750x+20.005

lnεSS=-QR1T+lnC

Solving for C,

lnC = 20.005

C = e20.005 min-1

Therefore, C=4.875x108 min-1

Solving for Q,

-QR=27750

Q=-R*-k

Q=-8.314 Jmol*K(-27750 K)

Q=2.30*105 J/mol

Therefore, Q=230 kJ/mol

(4A)

log(εss) = log(B) + nlog(σ)

y=m+kx

y= log(εss)	m= log(B)	k=n	x=log(σ)

(4B)

Figure 13. Plot of log steady state creep rate vs. log stress

(4C)

Figure 14. Plot of log steady state creep rate vs. log stress.

From Figure 14, the equation for the best fit line of the data is

y=1.3085x-6.4677

logεSS=nlogσ+logB

Solving for B,

logB=-6.4677

B=10^-6.4677

Therefore, B=0.015527

n=1.3085

(4D)

Figure 15. Plot of log stress versus the rupture time.

(5A)

Sample calculation:

The Larson-Miller Parameter is shown below in Equation (3).

L-M Parameter=T[C'+logtf]				(3)

For experiment #1,

L-M Parameter= (1223 K)*[20+log(1.2431)]

L-M Parameter= 24575.58

(5B)

Table 4. Table of Larson-Miller Parameter, temperature, time to failure, and stress.

| run | Temp(Kelvin) | Stress (Psi) | Log Stress (Psi) | Time To Rupture (hours) | Larson miller parameter |
| --- | --- | --- | --- | --- | --- |
| 1 | 1198 | 15636.63221 | 4.194143221 | 0.283333333 | 23303.85261 |
| 2 | 1223 | 15636.63221 | 4.194143221 | 0.163833333 | 23499.21397 |
| 3 | 1248 | 15636.63221 | 4.194143221 | 0.091666667 | 23664.83988 |
| 4 | 1248 | 13553.48822 | 4.132051083 | 0.091666667 | 23664.83988 |
| 5 | 1248 | 12524.9685 | 4.097776642 | 0.1305 | 23856.28192 |

(5C)

Figure 16. Larson-Miller parameter versus the log stress

Questions:

(1A)

Since εss=Bσn and εss=Aσnexp⁡(-QRT), set Bσn =Aσnexp⁡(-QRT)

Then, solve for A: A = Bexp⁡(-QRT)

Since εss=Aσnexp⁡(-QRT) and εss=C exp (-QRT), set Aσnexp-QRT = C exp (-QRT)

Then, solve for A: A = Cσn

(1B) Using the equation εss=C exp (-QRT) , with:

C = 4.875 x108

Q = 230 x103

T= 1073K

R = 8.314:

ss = 4.875 x108exp ((-230 x103)/(8.314*1073)) = 0.003097 min-1

(2) In 20 years, there are 175,200 hours.

T = LM(C'+log⁡(175,200hrs)

LM at lowest stress level = 23856.28192

T = 23856.28192/[20 + log(175200)] = 945 K

(3) With increasing stress or temperature, what changes will you notice in a typical creep curve?

Table 5. Whenever stress is increased while temperature is held constant, as in runs 3,4, and 5, I saw that the minimum slope, corresoponding to ss, in the graph shows an increase.  The time to rupture is increased as stress is increased.  Strain that the wire is able to achieve before rupture decreases as stress increases.

Temperature has a similar effect on ss, strain, and time to rupture. This trend can be seen in table 5. Runs 1, 2, and 3 illustrate the effects of increasing temperature and fixing stress. ss increases, and on the graph that shows up as a steeper slope. Time to rupture decreases.

Table 5. Temperature, stress, steady-state creep rate, and time to fracture

| Run | Temp (celsius) | Stress (Psi) | Steady-State Creep Rate (min.-1) | Time to Fracture (minutes) |
| --- | --- | --- | --- | --- |
| 1 | 925 | 15636.63221 | 0.039 | 17 |
| 2 | 950 | 15636.63221 | 0.0812 | 9.83 |
| 3 | 975 | 15636.63221 | 0.0983 | 5.5 |
| 4 | 975 | 13553.48822 | 0.1041 | 5.5 |
| 5 | 975 | 12524.9685 | 0.0698 | 7.83 |

(4) Does chromel have a well-defined secondary creep stage? Explain your answer.

Chromel does not have a well-defined secondary creep stage. Secondary creep state is characterized by a steady creep rate. The steady creep rate would appear as a line with constant slope. Chromel does not show this throughout all the runs.

(5) Creep data usually exhibit a large amount of scattering. How much scatter existed in your data? This can be estimated from graphs 3, 4, and 5 of the analysis section. Be specific in your answer.

In the creep curves there was not a lot of scatter. In fact, the the data is very close together. This is because the time intervals between taking measurements was either ever ten seconds or every five seconds. Everything was controlled very well so as to not mess effect the experiment.

(6) Put your sketch of the fractured specimen here, and describe the features shown.

Our TA said that there was no microscope so we did not have to do the sketch.

(7) Creep Deformation mechanisms all involve the diffusion of atoms, explaining increased transport at higher temperatures.

(A) What is diffusion and why does it occur?

Diffusion is when atoms move from an area of high concentration to an area of low concentration.  It occurs due to the internal energy that is inside the material. The energy wants to go to equilibrium.

(B) Why does it occur most rapidly at grain boundaries.

It occurs more rapidly at grain boundaries because there is more space for the atoms to move freely; it is less densely packed at grain boundaries.

(8) Primary creep is typified by a continuously decreasing creep rate. Give reasons.

Primary or transient creep occurs first, typified by a continuously decreasing creep rate—that is, the slope of the curve decreases with time. This suggests that the material is experiencing an increase in creep resistance or strain hardening deformation becomes more difficult as the material is strained.  (Book)

(9) Why is the creep rate constant during the secondary creep state? What causes the tertiary creep state to appear?

For secondary creep, sometimes termed steady-state creep, the rate is constant—that is, the plot becomes linear. This is often the stage of creep that is of the longest duration. The constancy of creep rate is explained on the basis of a balance between the competing processes of strain hardening and recovery, recovery being the process by which a material becomes softer and retains its ability to experience deformation.

Finally, for tertiary creep, there is an acceleration of the rate and ultimate failure. This failure could be from a number of reasons like, grain boundary separation, and the formation of internal cracks, cavities, and voids. Also, for tensile loads, a neck may form at some point within the deformation region. These all lead to a decrease in the effective cross-sectional area and an increase in strain rate.

(10) Give the approximate temperature at which creep deformation becomes an important consideration for each of the following metals; nickel, copper, and lead.

Creep deformation will begin to have effect on a metal when heated to temperatures greater than about 0.4Tm, where Tm is the absolute melting temperature. That being said, the melting temperatures (found on engineering tool box) of nickel, copper, and lead are: 1453 C, 1084 C, and 327.5 C respectively.

Sample calculation of when creep will occur for nickel: 0.4Tm(nickel)= 0.4*1453= 581.2 C

Temperature when creep will occur: Nickel: 581.2 C, Copper: 433.6 C, Lead: 131 C

(11) Steady-state creep data are given below for nickel at 200C. If it is known that the activation energy for creep is 140,000J/mol, compute the steady state creep rate at a temperature of 250C and a stress level of 48MPa (7000 psi).

ɛSS=Bσn

B=ɛSS1σ1n

n=lnɛSS2ɛSS1lnσ2σ1=ln⁡(24*10-225*10-3)ln55)=9.9736

B=ɛSS1σ1n=24*10-2699.974=1.0968*10-19

ɛSS=Bσn=1.0968*10-19*489.9736=0.006431 hour-1