# Analysis

The temperature, wire diameter, weight and stress for each test was recorded. This is shown below in Table I.

Table I: The temperature, wire diameter, mass, weight and stress for each test.

| Test | Temperature (°C) | Wire Diameter (mm) | Mass (kg) | Weight (N) | Stress (MPa) |
| --- | --- | --- | --- | --- | --- |
| 1 | 925 | 0.38608 | 1.498 | 14.69538 | 125.5267632 |
| 2 | 950 | 0.38608 | 1.498 | 14.69538 | 125.5267632 |
| 3 | 975 | 0.38608 | 1.498 | 14.69538 | 125.5267632 |
| 4 | 975 | 0.38608 | 1.2985 | 12.738285 | 108.8094139 |
| 5 | 975 | 0.38608 | 1.1995 | 11.767095 | 100.5135864 |

A sample calculation for stress is shown below.

σ=FA

Where, F is the weight and A is the cross sectional area of the wire. The data from Test 1 will be used to carry out the example.

σ=ForceArea=M1×9.81πD124=1.498×9.81[N]π0.3860824[mm2]=125.5267632 [MPa]

For each of the test a table was created showing time (in minutes), elongation, and strain. For this instance, it doesn’t matter if inches or millimeters are used for strain. The strain ratio will be the same as long as the units are consistent. For this reason the tables will continue to use the data in the units it was recorded, inches. Tables IIa though IIe contain the time, elongation and strain for the five test. These tables can be found below. To find strain the following equation was used.

ε=l-lolo=Elongation [in]5.95 [in]=0.0175.95=0.00286

Table IIa: The table for Test 1 containing time, elongation, and strain.

| Test 1 |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Time (min) | ΔL (in) | Strain | Time (min) | ΔL (in) | Strain | Time (min) | ΔL (in) | Strain |
| 0.000 | 0.000 | 0.00000 | 6.500 | 0.039 | 0.00655 | 13.000 | 0.079 | 0.01328 |
| 0.167 | 0.008 | 0.00134 | 6.667 | 0.039 | 0.00655 | 13.167 | 0.079 | 0.01328 |
| 0.333 | 0.014 | 0.00235 | 6.833 | 0.039 | 0.00655 | 13.333 | 0.079 | 0.01328 |
| 0.500 | 0.016 | 0.00269 | 7.000 | 0.043 | 0.00723 | 13.500 | 0.079 | 0.01328 |
| 0.667 | 0.017 | 0.00286 | 7.167 | 0.043 | 0.00723 | 13.667 | 0.080 | 0.01345 |
| 0.833 | 0.017 | 0.00286 | 7.333 | 0.045 | 0.00756 | 13.833 | 0.085 | 0.01429 |
| 1.000 | 0.017 | 0.00286 | 7.500 | 0.050 | 0.00840 | 14.000 | 0.085 | 0.01429 |
| 1.167 | 0.018 | 0.00303 | 7.667 | 0.050 | 0.00840 | 14.167 | 0.085 | 0.01429 |
| 1.333 | 0.018 | 0.00303 | 7.833 | 0.050 | 0.00840 | 14.333 | 0.085 | 0.01429 |
| 1.500 | 0.020 | 0.00336 | 8.000 | 0.050 | 0.00840 | 14.500 | 0.085 | 0.01429 |
| 1.667 | 0.022 | 0.00370 | 8.167 | 0.051 | 0.00857 | 14.667 | 0.085 | 0.01429 |
| 1.833 | 0.022 | 0.00370 | 8.333 | 0.056 | 0.00941 | 14.833 | 0.085 | 0.01429 |
| 2.000 | 0.022 | 0.00370 | 8.500 | 0.056 | 0.00941 | 15.000 | 0.086 | 0.01445 |
| 2.167 | 0.022 | 0.00370 | 8.667 | 0.056 | 0.00941 | 15.167 | 0.093 | 0.01563 |
| 2.333 | 0.023 | 0.00387 | 8.833 | 0.057 | 0.00958 | 15.333 | 0.093 | 0.01563 |
| 2.500 | 0.023 | 0.00387 | 9.000 | 0.058 | 0.00975 | 15.500 | 0.093 | 0.01563 |
| 2.667 | 0.024 | 0.00403 | 9.167 | 0.062 | 0.01042 | 15.667 | 0.094 | 0.01580 |
| 2.833 | 0.025 | 0.00420 | 9.333 | 0.062 | 0.01042 | 15.833 | 0.094 | 0.01580 |
| 3.000 | 0.026 | 0.00437 | 9.500 | 0.062 | 0.01042 | 16.000 | 0.094 | 0.01580 |
| 3.167 | 0.026 | 0.00437 | 9.667 | 0.062 | 0.01042 | 16.167 | 0.094 | 0.01580 |
| 3.333 | 0.026 | 0.00437 | 9.833 | 0.063 | 0.01059 | 16.333 | 0.094 | 0.01580 |
| 3.500 | 0.027 | 0.00454 | 10.000 | 0.063 | 0.01059 | 16.500 | 0.095 | 0.01597 |
| 3.667 | 0.029 | 0.00487 | 10.167 | 0.063 | 0.01059 | 16.667 | 0.095 | 0.01597 |
| 3.833 | 0.030 | 0.00504 | 10.333 | 0.063 | 0.01059 | 16.833 | 0.096 | 0.01613 |
| 4.000 | 0.030 | 0.00504 | 10.500 | 0.067 | 0.01126 | 17.000 | 0.097 | 0.01630 |
| 4.167 | 0.030 | 0.00504 | 10.667 | 0.068 | 0.01143 | 17.167 | 0.101 | 0.01697 |
| 4.333 | 0.030 | 0.00504 | 10.833 | 0.069 | 0.01160 | 17.333 | 0.101 | 0.01697 |
| 4.500 | 0.030 | 0.00504 | 11.000 | 0.069 | 0.01160 | 17.500 | 0.101 | 0.01697 |
| 4.667 | 0.030 | 0.00504 | 11.167 | 0.069 | 0.01160 | 17.667 | 0.101 | 0.01697 |
| 4.833 | 0.030 | 0.00504 | 11.333 | 0.069 | 0.01160 | 17.833 | 0.102 | 0.01714 |
| 5.000 | 0.030 | 0.00504 | 11.500 | 0.069 | 0.01160 | 18.000 | 0.108 | 0.01815 |
| 5.167 | 0.032 | 0.00538 | 11.667 | 0.071 | 0.01193 | 18.167 | 0.108 | 0.01815 |
| 5.333 | 0.032 | 0.00538 | 11.833 | 0.072 | 0.01210 | 18.333 | 0.109 | 0.01832 |
| 5.500 | 0.039 | 0.00655 | 12.000 | 0.072 | 0.01210 | 18.500 | 0.109 | 0.01832 |
| 5.667 | 0.039 | 0.00655 | 12.167 | 0.072 | 0.01210 | 18.667 | 0.109 | 0.01832 |
| 5.833 | 0.039 | 0.00655 | 12.333 | 0.072 | 0.01210 | 18.833 | 0.113 | 0.01899 |
| 6.000 | 0.039 | 0.00655 | 12.500 | 0.072 | 0.01210 | 19.000 | 0.113 | 0.01899 |
| 6.167 | 0.039 | 0.00655 | 12.667 | 0.074 | 0.01244 | 19.167 | 0.119 | 0.02000 |
| 6.333 | 0.039 | 0.00655 | 12.833 | 0.078 | 0.01311 | 19.333 | 0.119 | 0.02000 |
| 19.500 | 0.119 | 0.02000 | 26.000 | 0.173 | 0.02908 | 32.500 | 0.256 | 0.04303 |
| 19.667 | 0.124 | 0.02084 | 26.167 | 0.175 | 0.02941 | 32.667 | 0.260 | 0.04370 |
| 19.833 | 0.127 | 0.02134 | 26.333 | 0.182 | 0.03059 | 32.833 | 0.263 | 0.04420 |
| 20.000 | 0.127 | 0.02134 | 26.500 | 0.182 | 0.03059 | 33.000 | 0.264 | 0.04437 |
| 20.167 | 0.128 | 0.02151 | 26.667 | 0.182 | 0.03059 | 33.167 | 0.271 | 0.04555 |
| 20.333 | 0.128 | 0.02151 | 26.833 | 0.184 | 0.03092 | 33.333 | 0.275 | 0.04622 |
| 20.500 | 0.130 | 0.02185 | 27.000 | 0.184 | 0.03092 | 33.500 | 0.276 | 0.04639 |
| 20.667 | 0.134 | 0.02252 | 27.167 | 0.191 | 0.03210 | 33.667 | 0.276 | 0.04639 |
| 20.833 | 0.136 | 0.02286 | 27.333 | 0.191 | 0.03210 | 33.833 | 0.281 | 0.04723 |
| 21.000 | 0.136 | 0.02286 | 27.500 | 0.191 | 0.03210 | 34.000 | 0.283 | 0.04756 |
| 21.167 | 0.138 | 0.02319 | 27.667 | 0.191 | 0.03210 | 34.167 | 0.285 | 0.04790 |
| 21.333 | 0.139 | 0.02336 | 27.833 | 0.195 | 0.03277 | 34.333 | 0.292 | 0.04908 |
| 21.500 | 0.139 | 0.02336 | 28.000 | 0.197 | 0.03311 | 34.500 | 0.294 | 0.04941 |
| 21.667 | 0.141 | 0.02370 | 28.167 | 0.200 | 0.03361 | 34.667 | 0.295 | 0.04958 |
| 21.833 | 0.142 | 0.02387 | 28.333 | 0.201 | 0.03378 | 34.833 | 0.299 | 0.05025 |
| 22.000 | 0.142 | 0.02387 | 28.500 | 0.201 | 0.03378 | 35.000 | 0.307 | 0.05160 |
| 22.167 | 0.144 | 0.02420 | 28.667 | 0.201 | 0.03378 | 35.167 | 0.309 | 0.05193 |
| 22.333 | 0.144 | 0.02420 | 28.833 | 0.201 | 0.03378 | 35.333 | 0.310 | 0.05210 |
| 22.500 | 0.144 | 0.02420 | 29.000 | 0.205 | 0.03445 | 35.500 | 0.316 | 0.05311 |
| 22.667 | 0.144 | 0.02420 | 29.167 | 0.205 | 0.03445 | 35.667 | 0.321 | 0.05395 |
| 22.833 | 0.149 | 0.02504 | 29.333 | 0.206 | 0.03462 | 35.833 | 0.329 | 0.05529 |
| 23.000 | 0.149 | 0.02504 | 29.500 | 0.208 | 0.03496 | 36.000 | 0.338 | 0.05681 |
| 23.167 | 0.152 | 0.02555 | 29.667 | 0.220 | 0.03697 |  |  |  |
| 23.333 | 0.152 | 0.02555 | 29.833 | 0.221 | 0.03714 |  |  |  |
| 23.500 | 0.152 | 0.02555 | 30.000 | 0.221 | 0.03714 |  |  |  |
| 23.667 | 0.152 | 0.02555 | 30.167 | 0.221 | 0.03714 |  |  |  |
| 23.833 | 0.156 | 0.02622 | 30.333 | 0.222 | 0.03731 |  |  |  |
| 24.000 | 0.157 | 0.02639 | 30.500 | 0.222 | 0.03731 |  |  |  |
| 24.167 | 0.158 | 0.02655 | 30.667 | 0.223 | 0.03748 |  |  |  |
| 24.333 | 0.161 | 0.02706 | 30.833 | 0.227 | 0.03815 |  |  |  |
| 24.500 | 0.164 | 0.02756 | 31.000 | 0.227 | 0.03815 |  |  |  |
| 24.667 | 0.165 | 0.02773 | 31.167 | 0.227 | 0.03815 |  |  |  |
| 24.833 | 0.167 | 0.02807 | 31.333 | 0.236 | 0.03966 |  |  |  |
| 25.000 | 0.169 | 0.02840 | 31.500 | 0.239 | 0.04017 |  |  |  |
| 25.167 | 0.169 | 0.02840 | 31.667 | 0.247 | 0.04151 |  |  |  |
| 25.333 | 0.172 | 0.02891 | 31.833 | 0.249 | 0.04185 |  |  |  |
| 25.500 | 0.172 | 0.02891 | 32.000 | 0.251 | 0.04218 |  |  |  |
| 25.667 | 0.172 | 0.02891 | 32.167 | 0.251 | 0.04218 |  |  |  |
| 25.833 | 0.173 | 0.02908 | 32.333 | 0.252 | 0.04235 |  |  |  |

Table IIb: The table for Test 2 containing time, elongation, and strain.

| Test 2 |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Time (min) | ΔL (in) | Strain | Time (min) | ΔL (in) | Strain |
| 0.000 | 0 | 0.00000 | 4.333 | 0.193 | 0.03244 |
| 0.167 | 0.014 | 0.00235 | 4.500 | 0.204 | 0.03429 |
| 0.333 | 0.016 | 0.00269 | 4.667 | 0.213 | 0.03580 |
| 0.500 | 0.025 | 0.00420 | 4.833 | 0.215 | 0.03613 |
| 0.667 | 0.04 | 0.00672 | 5.000 | 0.223 | 0.03748 |
| 0.833 | 0.044 | 0.00739 | 5.167 | 0.24 | 0.04034 |
| 1.000 | 0.05 | 0.00840 | 5.333 | 0.255 | 0.04286 |
| 1.167 | 0.06 | 0.01008 | 5.500 | 0.265 | 0.04454 |
| 1.333 | 0.073 | 0.01227 | 5.667 | 0.269 | 0.04521 |
| 1.500 | 0.074 | 0.01244 | 5.833 | 0.274 | 0.04605 |
| 1.667 | 0.078 | 0.01311 | 6.000 | 0.294 | 0.04941 |
| 1.833 | 0.087 | 0.01462 | 6.167 | 0.298 | 0.05008 |
| 2.000 | 0.095 | 0.01597 | 6.333 | 0.313 | 0.05261 |
| 2.167 | 0.103 | 0.01731 | 6.500 | 0.319 | 0.05361 |
| 2.333 | 0.105 | 0.01765 | 6.667 | 0.332 | 0.05580 |
| 2.500 | 0.11 | 0.01849 | 6.833 | 0.351 | 0.05899 |
| 2.667 | 0.121 | 0.02034 | 7.000 | 0.37 | 0.06218 |
| 2.833 | 0.13 | 0.02185 | 7.167 | 0.38 | 0.06387 |
| 3.000 | 0.133 | 0.02235 | 7.333 | 0.389 | 0.06538 |
| 3.167 | 0.138 | 0.02319 | 7.500 | 0.405 | 0.06807 |
| 3.333 | 0.149 | 0.02504 | 7.667 | 0.421 | 0.07076 |
| 3.500 | 0.159 | 0.02672 | 7.833 | 0.439 | 0.07378 |
| 3.667 | 0.163 | 0.02739 | 8.000 | 0.462 | 0.07765 |
| 3.833 | 0.175 | 0.02941 | 8.167 | 0.49 | 0.08235 |
| 4.000 | 0.183 | 0.03076 | 8.333 | 0.52 | 0.08739 |
| 4.167 | 0.186 | 0.03126 |  |  |  |

Table IIc: The table for Test 3 containing time, elongation, and strain.

| Test 3 |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Time (min) | ΔL (in) | Strain | Time (min) | ΔL (in) | Strain |
| 0.000 | 0 | 0 | 1.933 | 0.165 | 0.02773109 |
| 0.067 | 0.02 | 0.00336134 | 2.000 | 0.173 | 0.02907563 |
| 0.133 | 0.025 | 0.00420168 | 2.067 | 0.177 | 0.0297479 |
| 0.200 | 0.033 | 0.00554622 | 2.133 | 0.182 | 0.03058824 |
| 0.267 | 0.037 | 0.00621849 | 2.200 | 0.187 | 0.03142857 |
| 0.333 | 0.04 | 0.00672269 | 2.267 | 0.195 | 0.03277311 |
| 0.400 | 0.046 | 0.00773109 | 2.333 | 0.202 | 0.03394958 |
| 0.467 | 0.052 | 0.0087395 | 2.400 | 0.208 | 0.03495798 |
| 0.533 | 0.059 | 0.00991597 | 2.467 | 0.214 | 0.03596639 |
| 0.600 | 0.064 | 0.0107563 | 2.533 | 0.22 | 0.03697479 |
| 0.667 | 0.07 | 0.01176471 | 2.600 | 0.225 | 0.03781513 |
| 0.733 | 0.071 | 0.01193277 | 2.667 | 0.233 | 0.03915966 |
| 0.800 | 0.074 | 0.01243697 | 2.733 | 0.239 | 0.04016807 |
| 0.867 | 0.078 | 0.01310924 | 2.800 | 0.245 | 0.04117647 |
| 0.933 | 0.081 | 0.01361345 | 2.867 | 0.253 | 0.04252101 |
| 1.000 | 0.088 | 0.01478992 | 2.933 | 0.263 | 0.04420168 |
| 1.067 | 0.095 | 0.01596639 | 3.000 | 0.268 | 0.04504202 |
| 1.133 | 0.1 | 0.01680672 | 3.067 | 0.273 | 0.04588235 |
| 1.200 | 0.108 | 0.01815126 | 3.133 | 0.282 | 0.04739496 |
| 1.267 | 0.113 | 0.0189916 | 3.200 | 0.287 | 0.04823529 |
| 1.333 | 0.114 | 0.01915966 | 3.267 | 0.292 | 0.04907563 |
| 1.400 | 0.118 | 0.01983193 | 3.333 | 0.303 | 0.05092437 |
| 1.467 | 0.123 | 0.02067227 | 3.400 | 0.309 | 0.05193277 |
| 1.533 | 0.128 | 0.02151261 | 3.467 | 0.316 | 0.05310924 |
| 1.600 | 0.131 | 0.02201681 | 3.533 | 0.328 | 0.05512605 |
| 1.667 | 0.137 | 0.02302521 | 3.600 | 0.333 | 0.05596639 |
| 1.733 | 0.15 | 0.02521008 | 3.667 | 0.344 | 0.05781513 |
| 1.800 | 0.155 | 0.02605042 | 3.733 | 0.353 | 0.05932773 |
| 1.867 | 0.16 | 0.02689076 |  |  |  |

Table IId: The table for Test 4 containing time, elongation, and strain.

| Test 4 |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Time (min) | ΔL (in) | Strain | Time (min) | ΔL (in) | Strain | Time (min) | ΔL (in) | Strain |
| 0.000 | 0 | 0.00000 | 2.533 | 0.126 | 0.02118 | 5.067 | 0.305 | 0.05126 |
| 0.067 | 0.01 | 0.00168 | 2.600 | 0.129 | 0.02168 | 5.133 | 0.313 | 0.05261 |
| 0.133 | 0.015 | 0.00252 | 2.667 | 0.13 | 0.02185 | 5.200 | 0.32 | 0.05378 |
| 0.200 | 0.016 | 0.00269 | 2.733 | 0.133 | 0.02235 | 5.267 | 0.331 | 0.05563 |
| 0.267 | 0.018 | 0.00303 | 2.800 | 0.139 | 0.02336 | 5.333 | 0.342 | 0.05748 |
| 0.333 | 0.019 | 0.00319 | 2.867 | 0.139 | 0.02336 | 5.400 | 0.352 | 0.05916 |
| 0.400 | 0.019 | 0.00319 | 2.933 | 0.142 | 0.02387 | 5.467 | 0.362 | 0.06084 |
| 0.467 | 0.023 | 0.00387 | 3.000 | 0.144 | 0.02420 | 5.533 | 0.374 | 0.06286 |
| 0.533 | 0.03 | 0.00504 | 3.067 | 0.148 | 0.02487 | 5.600 | 0.383 | 0.06437 |
| 0.600 | 0.032 | 0.00538 | 3.133 | 0.152 | 0.02555 | 5.667 | 0.412 | 0.06924 |
| 0.667 | 0.036 | 0.00605 | 3.200 | 0.154 | 0.02588 |  |  |  |
| 0.733 | 0.041 | 0.00689 | 3.267 | 0.16 | 0.02689 |  |  |  |
| 0.800 | 0.046 | 0.00773 | 3.333 | 0.17 | 0.02857 |  |  |  |
| 0.867 | 0.048 | 0.00807 | 3.400 | 0.172 | 0.02891 |  |  |  |
| 0.933 | 0.049 | 0.00824 | 3.467 | 0.174 | 0.02924 |  |  |  |
| 1.000 | 0.049 | 0.00824 | 3.533 | 0.179 | 0.03008 |  |  |  |
| 1.067 | 0.049 | 0.00824 | 3.600 | 0.186 | 0.03126 |  |  |  |
| 1.133 | 0.053 | 0.00891 | 3.667 | 0.189 | 0.03176 |  |  |  |
| 1.200 | 0.057 | 0.00958 | 3.733 | 0.191 | 0.03210 |  |  |  |
| 1.267 | 0.057 | 0.00958 | 3.800 | 0.194 | 0.03261 |  |  |  |
| 1.333 | 0.057 | 0.00958 | 3.867 | 0.197 | 0.03311 |  |  |  |
| 1.400 | 0.063 | 0.01059 | 3.933 | 0.204 | 0.03429 |  |  |  |
| 1.467 | 0.068 | 0.01143 | 4.000 | 0.206 | 0.03462 |  |  |  |
| 1.533 | 0.07 | 0.01176 | 4.067 | 0.212 | 0.03563 |  |  |  |
| 1.600 | 0.08 | 0.01345 | 4.133 | 0.215 | 0.03613 |  |  |  |
| 1.667 | 0.083 | 0.01395 | 4.200 | 0.219 | 0.03681 |  |  |  |
| 1.733 | 0.087 | 0.01462 | 4.267 | 0.226 | 0.03798 |  |  |  |
| 1.800 | 0.088 | 0.01479 | 4.333 | 0.232 | 0.03899 |  |  |  |
| 1.867 | 0.091 | 0.01529 | 4.400 | 0.241 | 0.04050 |  |  |  |
| 1.933 | 0.095 | 0.01597 | 4.467 | 0.247 | 0.04151 |  |  |  |
| 2.000 | 0.1 | 0.01681 | 4.533 | 0.251 | 0.04218 |  |  |  |
| 2.067 | 0.103 | 0.01731 | 4.600 | 0.258 | 0.04336 |  |  |  |
| 2.133 | 0.109 | 0.01832 | 4.667 | 0.262 | 0.04403 |  |  |  |
| 2.200 | 0.113 | 0.01899 | 4.733 | 0.269 | 0.04521 |  |  |  |
| 2.267 | 0.114 | 0.01916 | 4.800 | 0.275 | 0.04622 |  |  |  |
| 2.333 | 0.115 | 0.01933 | 4.867 | 0.283 | 0.04756 |  |  |  |
| 2.400 | 0.115 | 0.01933 | 4.933 | 0.29 | 0.04874 |  |  |  |
| 2.467 | 0.119 | 0.02000 | 5.000 | 0.297 | 0.04992 |  |  |  |

Table IIe: The table for Test 5 containing time, elongation, and strain.

| Test 5 |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Time (min) | ΔL (in) | Strain | Time (min) | ΔL (in) | Strain |
| 0.000 | 0 | 0.00000 | 2.400 | 0.136 | 0.02286 |
| 0.067 | 0.012 | 0.00202 | 2.467 | 0.14 | 0.02353 |
| 0.133 | 0.015 | 0.00252 | 2.533 | 0.145 | 0.02437 |
| 0.200 | 0.018 | 0.00303 | 2.600 | 0.147 | 0.02471 |
| 0.267 | 0.022 | 0.00370 | 2.667 | 0.144 | 0.02420 |
| 0.333 | 0.025 | 0.00420 | 2.733 | 0.157 | 0.02639 |
| 0.400 | 0.026 | 0.00437 | 2.800 | 0.163 | 0.02739 |
| 0.467 | 0.03 | 0.00504 | 2.867 | 0.166 | 0.02790 |
| 0.533 | 0.032 | 0.00538 | 2.933 | 0.17 | 0.02857 |
| 0.600 | 0.036 | 0.00605 | 3.000 | 0.175 | 0.02941 |
| 0.667 | 0.041 | 0.00689 | 3.067 | 0.18 | 0.03025 |
| 0.733 | 0.042 | 0.00706 | 3.133 | 0.186 | 0.03126 |
| 0.800 | 0.046 | 0.00773 | 3.200 | 0.191 | 0.03210 |
| 0.867 | 0.052 | 0.00874 | 3.267 | 0.199 | 0.03345 |
| 0.933 | 0.055 | 0.00924 | 3.333 | 0.202 | 0.03395 |
| 1.000 | 0.06 | 0.01008 | 3.400 | 0.208 | 0.03496 |
| 1.067 | 0.065 | 0.01092 | 3.467 | 0.212 | 0.03563 |
| 1.133 | 0.068 | 0.01143 | 3.533 | 0.217 | 0.03647 |
| 1.200 | 0.075 | 0.01261 | 3.600 | 0.223 | 0.03748 |
| 1.267 | 0.077 | 0.01294 | 3.667 | 0.231 | 0.03882 |
| 1.333 | 0.078 | 0.01311 | 3.733 | 0.239 | 0.04017 |
| 1.400 | 0.085 | 0.01429 | 3.800 | 0.25 | 0.04202 |
| 1.467 | 0.086 | 0.01445 | 3.867 | 0.252 | 0.04235 |
| 1.533 | 0.087 | 0.01462 | 3.933 | 0.259 | 0.04353 |
| 1.600 | 0.09 | 0.01513 | 4.000 | 0.265 | 0.04454 |
| 1.667 | 0.093 | 0.01563 | 4.067 | 0.273 | 0.04588 |
| 1.733 | 0.097 | 0.01630 | 4.133 | 0.281 | 0.04723 |
| 1.800 | 0.1 | 0.01681 | 4.200 | 0.288 | 0.04840 |
| 1.867 | 0.104 | 0.01748 | 4.267 | 0.297 | 0.04992 |
| 1.933 | 0.107 | 0.01798 | 4.333 | 0.308 | 0.05176 |
| 2.000 | 0.112 | 0.01882 | 4.400 | 0.32 | 0.05378 |
| 2.067 | 0.116 | 0.01950 | 4.467 | 0.335 | 0.05630 |
| 2.133 | 0.12 | 0.02017 | 4.533 | 0.355 | 0.05966 |
| 2.200 | 0.125 | 0.02101 | 4.600 | 0.37 | 0.06218 |
| 2.267 | 0.129 | 0.02168 | 4.667 | 0.378 | 0.06353 |
| 2.333 | 133 | 22.35294 |  |  |  |

The creep curves needed to be plotted for each test. These plots are shown below.

Figure 1: The creep curve for Test 1.

Figure 2: The creep curve for Test 2.

Figure 3: The creep curve for Test 3.

Figure 4: The creep curve Test 4.

Figure 5: The creep curve for Test 5.

Table III: The stress, temperature, creep rate and final time for the five trials.

| Test | Stress (MPa) | Temperature (°C) | εss | Tf (min) |
| --- | --- | --- | --- | --- |
| 1 | 125.5267632 | 925 | 0.0014 | 36 |
| 2 | 125.5267632 | 950 | 0.0076 | 8.333 |
| 3 | 125.5267632 | 975 | 0.0153 | 3.73 |
| 4 | 108.8094139 | 975 | 0.0078 | 5.000 |
| 5 | 100.5135864 | 975 | 0.0098 | 4.667 |

The equation,y=kx+m, is a variation of Equation 2 from the lab manual. This is shown below.

εss=Ce-QRT

lnεssC=-QRT

lnεss-lnC=-QRT

lnεss=-QR1T+lnC

Where,

y= lnεss

k= -QR

x= 1T

m=lnC=C

Which results in,

y=kx+m

This relation can be observed with the various test data. A plot of the lnεss vs T-1 is shown below in Figure 6.

Figure 6: The linear relation between creep rate and temperature for points with constant stress.

The values for C and Q can be determined from the linear relation. This is shown below.

-71717x+53.439=-QR1T+ lnC

-QR=-71717

Q=71717K*8.31Jmol*K=595.97KJmol

lnC=53.439

C=e53.439=1.62×1023

It can also be shown that Equation 1 from the lab manual can be written as y=kx+m. This is shown below.

εss=Bσn

logεss=nlog⁡(σ)+ log⁡(B)

y=kx+m

Where,

y= logεss

k= n

x= log⁡(σ)

m=log⁡(B)

This can also be seen through Figure 7, below.

Figure 7: The plot of logarithmic strain rate and stress.

Logarithmic stress was plotted against rupture time. This is shown in Figure 8. Due to inconsistencies, the experimental results do not match the expected results.

Figure 8: Logarithmic stress against the rupture time.

The Larson-Miller Parameter for each test is recorded below in Table IV. An example of calculating the L-M Parameter is also shown.

Table IV: The L-M parameter for the five test.

| Test | Stress (MPa) | Temperature (°C) | Tf (min) | L-M Parameter |
| --- | --- | --- | --- | --- |
| 1 | 125.5267632 | 925 | 36 | 23697.19192 |
| 2 | 125.5267632 | 950 | 8.333 | 23414.33251 |
| 3 | 125.5267632 | 975 | 3.73 | 23457.1789 |
| 4 | 108.8094139 | 975 | 5 | 23616.01993 |
| 5 | 100.5135864 | 975 | 4.667 | 23578.66005 |

For the sample calculation, the value of 20 was assumed for the C’ variable. Temperature was also converted to Kelvin.

L-M Parameter=TC'+logTf

L-M Parameter=(925+273.15)20+log3660

L-M Parameter=23697.192

A plot for the L-M Parameter versus log(σ) was made. This is shown in Figure 9 below.

Figure 9: The L-M parameters plotted against logarithmic stress.

# Questions

  - Show that

A=Be-QRT

And that

A=Cσn

We know,

εss=Ce-QRT

εss=Bσn

εss=Aσne-QRT

Rearrange to get,

A=εssσne-QRT

Substituting for εss,

A=Bσnσne-QRT	 and	 A=Ce-QRTσne-QRT

Which reduce to,

A=Be-QRT 	and	A=Cσn

  - What value of creep rate would you expect at 800°C and 16000 psi?

Using,

εss=Ce-QRT

εss=1.62×1023e-5959708.31×800+273.15=1.535×10-6

- Using your Larson-Miller curve, what temperature should you use for a life of 20 years at the lowest stress level?

Tf=20yrs=175200hrs

L-M Parameter=23697.192

L-M Parameter=TC'+logTf

T=L-M ParameterC'+logTf

T=23697.19220+log175200

T=938.74 K

- With increasing stress or temperature, what changes will you notice in a typical creep curve?

As temperature increases, strain will increase. However, the rupture time will decrease. This is reinforced by the data in Table III. As stress increases, strain will increase while rupture time decreases. There is an inconsistency that prevents this from being seen

- Does chromel have a well-defined secondary creep stage? Explain your answer.

The secondary creep stage is not well-defined. The five creep curves flow relatively smoothly except for when we reach the tertiary creep stage. The primary and secondary stages are similar and it is difficult to distinguish between the two. Since the two can’t be distinguished, it can be said that the secondary stage is not well defined.

- Creep data usually exhibit a large amount of scattering. How much scatter existed in your data? This can be estimated from your graphs in 3, 4 and 5 of the analysis section. Be specific in your answer.

The scatter amount experienced was not large. Looking at the creep curves, the data follows a relatively smooth curve. There are small bumps along the curve but not enough to prevent the students from understanding what the general trend of the creep curve is. These small deviations can be a result of many things, including human errors and inconsistencies, as seen with Test 5.

- Put your sketch of the fractured specimen here, and describe the features shown.

The group was not instructed to observe or record the specimen samples.

- Creep deformation mechanisms all involve the diffusion of atoms, explaining increased transport at higher temperatures. What is diffusion and how does it occur? Why does it occur most rapidly at grain boundaries?

Diffusion is when atoms move within the structure. The diffusion occurs through many reasons, some which include diffusion of atoms through vacancies, and even temperature. With vacancies atoms move to an empty location. An increase in temperature will increase the movement of the atoms, allowing for greater diffusion. Diffusion happens much faster along grain boundaries because of any defects present on the surface.

- Primary creep is typified by a continuously decreasing creep rate. Give reasons.

Strain hardening occurs in the primary stage. Strain hardening results in a stronger material that resists elongation. Strain is a measurement of elongation, and if there is a resistance to it, the creep rate will decrease.

- Why is the creep rate constant during the secondary creep state? What causes the tertiary creep state to appear? [Hint: Use the effect of both strain hardening and the creep damage to the microstructure].

In the secondary stage, we no longer see strain hardening which means there is no longer the initial resistance to elongation. This is because our sample reached a uniform temperature throughout. With strain hardening gone and a uniform temperature, it is possible for the creep rate to stay constant.

The tertiary stage occurs because of the separation that occurs along the grain boundaries. As mentioned earlier, diffusion occurs faster along the grain boundaries, so as time goes on, our sample begins to elongate at an exponential rate. An example of this was when the dial would begin to jump around whenever the sample was close to fracture. This rate continues up until the fracture point.

- Give the approximate temperature at which creep deformation becomes an important consideration for each of the following metals; nickel, copper and lead.

Creep becomes important around 0.4Tm. Where Tm is the melting temperature. Using a reference to find the melting temperature for these metals we can find the temperature for creep.

For Ni:

Tm=1728.15

0.4Tm=1728.15×0.4=691.26

Cu:

0.4Tm=1358.15×0.4=543.26

Pb:

0.4Tm=600.15×0.4=240.06

- Steady-state creep rate data are given for nickel at 200 °C. If it is known that the activation energy for creep is 140,000 J/mol, compute the steady-state creep rate at a temperature of 250 °C and a stress level of 48 MPa (7000 psi).

εss=Bσn

logεss=nlog⁡(σ)+ log⁡(B)

log24×10-2=nlog⁡(69)+ log⁡(B)

log25×10-3=nlog55+logB

Substituting log(B),

log25×10-3=nlog55+log24×10-2-nlog(69)

n=log25x10-324x10-2log5569

n=9.974

Solving for log(B),

log⁡(B)=log25x10-3-9.974log⁡(55)

B=1.0954×10-19

Substituting back into the creep rate equation,

εss=Bσn=1.0954x10-19(48)9.974=6.43×10-31hours