Conclusions

In the current study, the effect of angular deviation out of plane angle β and in plane angle α on magnetic domain structure and magnetic performance were investigated. It was evident that even with deviation as high as 2.8° or even 6.1° out of plan, β, the sample did not have any supplementary. The reason why it did not show any supplementary domain is that they are usually found in beta angle of 1 degree or higher but our case there was none.  Also, the grain boundary mis-orientation angle have  influence on the continuation or transfer of the magnetic pattern. This is where low angle grain boundary seen permitting the pattern to pass undisturbed between adjacent grains. The majority of grain boundaries in samples with lower magnetic performance are high grain boundaries, in which it might be contributing in higher magnetic losses. Statistical tools used for orientation quality comparison, linking range of distribution and deviation from the average angular deviation to magnetic performance. Samples with tight distribution around low average value and lower distribution range have better magnetic losses and permeability.

The sample thickness leads to the magnetic performance due to larger Eddy loss specially thicker grades, while slightly thicker sample 0.27mm, can outperform thinner samples 0.23mm with tight distribution around the average angular deviation and lower distribution range.

References

[1]	A. Morawiec, “On abnormal growth of Goss grains in grain-oriented silicon steel,” Scr. Mater., vol. 64, no. 5, pp. 466–469, 2011.

[2]	J. W. Shilling and G. L. Houze, “Magnetic Properties and Domain Structure in Grain-Oriented 3% Si-Fe,” IEEE Trans. Magn., vol. 10, no. 2, pp. 195–223, 1974.

[3]	A. a Almeida, D. L. Rodrigues-jr, L. S. P. Perassa, J. Leicht, and F. J. G. Landgraf, “Anomalous Loss Hysteresis Loop,” Mater. Res., vol. 17, no. 2, pp. 3–6, 2014.

[4]	D. Dorner, S. Zaefferer, L. Lahn, and D. Raabe, “Overview of Microstructure and Microtexture Development in Grain-oriented Silicon Steel,” J. Magn. Magn. Mater., vol. 304, no. 2, pp. 183–186, 2006.

[5]	T. Kubota, M. Fujikura, and Y. Ushigami, “Recent progress and future trend on grain-oriented silicon steel,” J. Magn. Magn. Mater., vol. 215, pp. 69–73, 2000.

[6]	C. Gheorghies and A. Doniga, “Evolution of Texture in Grain Oriented Silicon Steels,” J. Iron Steel Res. Int., vol. 16, no. 4, pp. 78–83, 2009.

[7]	M. Matsuo, “Review Texture Control in the Production of Grain Oriented Silicon Steels Grain Oriented Silicon Steels Texture Control for Improved Magnetic Properties,” ISII Int., vol. 29, no. lO, pp. 809–827, 1989.

[8]	Y. Ushigami, M. Mizokami, M. Fujikura, T. Kubota, H. Fujii, and K. Murakami, “Recent development of low-loss grain-oriented silicon steel,” J. Magn. Magn. Mater., vol. 254–255, pp. 307–314, 2003.

[9]	N. Takahashi, Y. Suga, and H. Kobayashi, “Recent developments in grain-oriented silicon-steel,” J. Magn. Magn. Mater., vol. 160, pp. 98–101, 1996.

[10]	M. Imamura and T. Sasaki, “The status of domain theory for an investigation of magnetostriction and magnetization processes in grain-oriented si-fe sheets,” Phys. Scr., vol. 1988, no. T24, pp. 29–35, 1988.

[11]	M. Imamura, S. Tadashi, and A. Saito, “Magnetization Process and Magnetostriction of a 4% Si-Fe single crystal close to (110)[001],” Ieee, vol. M, no. 5, 1981.

[12]	T. Nozawa, M. Mizogami, H. Mogi, and Y. Matsuo, “Magnetic properties and dynamic domain behavior in grain-oriented 3 % Si-Fe,” IEEE Trans. Magn., vol. 32, no. 2, pp. 572–589, 1996.

[13]	S. Chikazumi and C. D. Graham, Physics of Ferromagnetism 2e, vol. 94. Oxford University Press on Demand, 2009.

[14]	A. Hubert and R. Schäfer, Magnetic domains: the analysis of magnetic microstructures. Springer Science & Business Media, 2008. city??

[15]	M. Gallaugher, N. Brodusch, R. Gauvin, and R. R. Chromik, “Magnetic domain structure and crystallographic orientation of electrical steels revealed by a forescatter detector and electron backscatter diffraction,” Ultramicroscopy, vol. 142, pp. 40–49, 2014.

[16]	T. Yamamoto, H. Nishizawa, and K. Tsuno, “High voltage scanning electron microscopy for observing magnetic domains,” J. Phys. D. Appl. Phys., vol. 8, no. 9, pp. 18–21, 1975.

[17]	N. Bernier, E. Leunis, C. Furtado, T. Van De Putte, and G. Ban, “EBSD study of angular deviations from the Goss component in grain-oriented electrical steels,” Micron, vol. 54–55, pp. 43–51, 2013.

[18]	H. Bunge, Texture analysis in materials science : mathematical methods. Butterworths, 1982. city??/

[19]	V. Randle and O. Engler, Introduction to Texture analysis: Macrotexture, Microtexture & Orientation Mapping. 2000., city??

[20]	W. S. Paxton and T. G. Nilan, “Domain configurations and crystallographic orientation in grain-oriented silicon steel,” J. Appl. Phys., vol. 26, no. 8, pp. 994–1000, 1955.

[21]	S. Shin, R. Schafer, and B. C. De Cooman, “Grain boundary penetration by lancet domains in Fe-3%Si grain-oriented steel,” IEEE Trans. Magn., vol. 46, no. 9, pp. 3574–3581, 2010.

[22]	L. J. Dijkstra and U. M. Martius, “Domain pattern in silicon-iron under stress,” Rev. Mod. Phys., vol. 25, no. 1, pp. 146–150, 1953.

[23]	O. Perevertov and R. Schäfer, “Magnetic properties and magnetic domain structure of grainoriented Fe-3%Si steel under compression,” Mater. Res. Express, vol. 3, no. 9, pp. 1–12, 2016.

[24]	M. McCarty, G. L. Houze, and F. A. Malagari, “Texture-Electrical-Property Correlations in Oriented Silicon Steel,” J. Appl. Phys., vol. 38, no. 3, pp. 1096–1098, 1967.

[25]	Z. Xia, Y. Kang, and Q. Wang, “Developments in the production of grain-oriented electrical steel,” J. Magn. Magn. Mater., vol. 320, no. 23, pp. 3229–3233, 2008.