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Abstract
[bookmark: _GoBack]Most of the aluminium alloys that are extruded have some mechanical properties that are anisotropic. In this report, the strain-stress behavior of aluminium 7075 alloys was experimented using a tensile machine. The experiment was conducted in three different directions which were in respect to the extrusion behaviors. The experiment was conducted to analyze the mechanical properties of heated aluminium alloy and the discussion about their comparison were made from the values extruded from the tensile machine. In the experiment, cross arm displacement and extensometer displacement were the methods that were used to collect data from the aluminium alloy accurately.
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Tensile Testing
Introduction
Aluminium alloys have many engineering applications due to their mechanical and structural properties. The aluminium alloys are light and have the crashworthy capabilities which are preferred in most of the automotive industries. The alloys have high strength and are light which is then used in most of the aerospace design and manufacturing. Therefore, the increased number of manufacturing designs of these aluminium alloys have made it necessary to have better testing material models where they are perfectly studied with perfection and coefficients involved in the material model are carefully identified.
There are some investigators who have conducted aluminium alloy test. At room temperature, Oosterkamp et al. (1999) conducted a compression test at aluminium 7075 that resulted in a small increase in the stress flow concerning the strain rate. Reyes et al. (2006) experimented using other alloys of aluminium 7075 and go similar sensitivity observation. Børvik et al. (2005) conducted the flow stress and structure strain where the results showed a strong and positive sensitivity on the strain rate. El-Magd and Abouridouane (2006) did the tension test, and the result showed that the flow stress increases slightly with the strain rate. However, the increasing rates at deformation decreased in tension and increased in tension. When Clausen et al. (2004) measured the fracture strains at different strain rates in all tension tests, the results were such that the fracture strains is independent in the dynamic strain regime where it increases considerably at higher rates. 
Therefore, to calculate these stress-strain analyses, different formulas were used which are:
Ϭ=S (1+ δ)
ℰ= ln (1+ δ)

Where 
· Ϭ=true stress
· δ= engineering strain
· ℰ= true strain
· S=engineering stress
Objectives
· To determine the yield strength, ultimate tensile strength, and elongation for aluminum samples in two different heat treat conditions
· To compare the use of crosshead and extensometer displacement measurements 
· To examine how cold working increases the strength of an aluminum alloy 

Procedure
	One 7075 Aluminium specimen that was cold worked and two 7075 aluminium that were heat treated by annealing them in the air for three hours at 415 °C. Literature data of the mechanical properties; tensile strength, yield strength and ductility of the specimens were derived from the textbox's appendix. The data was used to generate functions of engineering stress against engineering strain. 
Drawbacks
The tensile test machine is very expensive, with its price being not less than $10000. Furthermore, the machine is susceptible to failure in case of overload.
 Before the tensile test was done, the load cell rated maximum capacity was checked so as not to overload the system. The highest tensile strength that the machine could tolerate was calculated by dividing the cross-sectional area of the gage length of the test specimen. 
 A spreadsheet containing time, load, crossarm extension and extensometer displacement was created based on the tensile test data generated by the loading cell machines software. This data was used to generate experimental graphs of engineering stress and strain. Comparisons of the experimental data and literature data were made. Also, differences between the extensometer displacement and crossarm displacement were studied.
 The following formulas were used to generate additional data;
P   = load          
 Ao = initial cross-sectional area of the specimen           
 s   = engineering stress = P / Ao 
Lo = gauge length measured on the specimen (4 inches)      
 ∆ L = crossarm extension          
e1 = engineering strain measured from the crossarm displacement = ∆ L / Lo       
L20 = extensometer knife edge separation before tensile test (2 inches)             
L2   = extensometer knife edge separation at any time during the tensile test             
 e2 = engineering strain measured from the extensometer = (L2 - L20) / L20 
True stress and strain were also calculated. 
A = instantaneous cross-sectional area of the specimen    
σ = true stress = P/A = s (e2 + 1)      
ε 1 = true strain measured by crossarm displacement = ln [(∆ L + L0)/L0] = ln (e1 + 1)     
 ε 2 = true strain measured by extensometer = ln (L2/L20) = ln (e2 + 1) 
	The test was done in four phases. The first specimen, cold worked 7075 aluminium, was loaded to failure and the results labeled as sample1. The second specimen annealed aluminium was loaded to failure.in the third test, annealed 7075 aluminium specimen was work harden by loading it above its yield point. This was referred to as sample 3. The specimen was then loaded again but to failure. This was sample4. The results from the four tests were used to generate graphs and values of Young's modulus yield strength, ultimate strength, stress, and strain were obtained.











Results and Discussions
Results from the cold worked 7075 aluminium which was loaded to failure are in the table below.


Table 1 sample 1 results


Table 2 sample 2 results


Table 3 sample 3 results


Table 4 sample 4 results

Figure 1 strain verse stress for sample 1 and sample2

The above is a plot of two curves:  σ as a function ε 2 for sample1 and sample2. Cold worked aluminium has lower yield strength compared to annealed samples. However, annealed aluminium has superior strain hardening qualities. The fact that annealing involves heating the material under considerably high temperatures, a uniform lattice is formed as it cools thus minimizing the internal stress and cracks. Therefore, it has higher yield strength and higher strain-to-fracture ratio due to minimized internal stresses. It also can withstand higher ultimate load.

Figure 2 true stress verses true strain
Sample 4 offers the highest yield strength in comparison to the other specimen. This is because majorly annealed aluminum 7075 specimen was work hardened (sample 3) before the final experiment. This increased its yield strength at the expense of its strain hardening strength. Sample 3 offers higher yield strength as compared to sample 2 as well as strain hardening.
 	Meanwhile, sample3 exhibited higher ultimate strength and strain-to-failure in comparison to the other samples. This is due to the fact that it does not undergo any prior loading, therefore, there is minimal internal stress within the sample.

Figure 3 stress and trues stress verse strain graph
	The true stress being a function of engineering stress, the two graphs do not cross at zero. The two stresses are proportional to each other.
.
Figure 4 strain verse engineering stress of sample 1
Young’s modulus (crossarm displacement);

Young” modulus (extensometer displacement);

Crossarm displacement, e1 gives a more accurate value than the extensometer. Extensometer takes a recording of the average displacement. This explains why its values are less compared to the cross arm displacement method. In addition, calibration of the extensometer is rather difficult.
The literature values differ from the experimental data values. This is because experimental data is inclusive of the defects within the specimen while the literature data assumes the specimen has zero defects. These defects mainly occur during the manufacturing process.
CONCLUSION
Finite element software was used to conduct a test on four pieces of aluminium 7075 and determine their stress-strain relationships. Graphs from the data generated by the machine were used to plot graphs which aided in analyzing the mechanical properties of the specimens. Careful recording and reading of measurement and well calibrated gauges can reduce errors in the experiment.
EXPERIMENTAL ERRORS
Errors in the results from the data obtained could be due to faulty loading machine; machine flexes, measurement recording errors and calibration errors.
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STRESS VS STRAIN FOR SAMPLE 1 AND 2
LOAD (N) (p)	101.6	156.57288700000001	1301.762326	3959.0782669999999	7927.6525389999997	12889.601971	17826.396718	22319.823516	23299.844714999999	23619.530568999999	23859.556527000001	24040.888616	24163.522048999999	24226.41056	23963.323646000001	stress 2	85.801689999999994	4387.2481189999999	8324.9021670000002	11440.532612000001	13032.151576	14125.37305	14974.376319000001	15717.515148	16352.695806	16896.686088999999	17368.354704000001	17754.073853999998	18085.290185999998	18362.002505	18586.306933	18767.636628	18910.185035999999	19013.952154999999	18947.918860000002	18631.376593000001	STRESS
TRUE STRESS VERSES TRUE STRAIN

stress 2	0	1	2.0074999999999998	3.0150000000000001	4.0075000000000003	5.03	6.0025000000000004	7.0049999999999999	8.0075000000000003	9.01	10.032500000000001	11.0175	12.022500000000001	13.0275	14.03	15.012499999999999	16.014999	17.02	18.024999999999999	18.389999	85.801689999999994	4387.2481189999999	8324.9021670000002	11440.532612000001	13032.151576	14125.37305	14974.376319000001	15717.515148	16352.695806	16896.686088999999	17368.354704000001	17754.073853999998	18085.290185999998	18362.002505	18586.306933	18767.636628	18910.185035999999	19013.952154999999	18947.918860000002	18631.376593000001	stress 3	0	1	2.0074999999999998	3.0150000000000001	4.0075000000000003	5.03	6.0025000000000004	7.0049999999999999	8.0075000000000003	9.01	10.032500000000001	11.0175	12.022500000000001	13.0275	14.03	15.012499999999999	16.014999	17.02	18.024999999999999	18.389999	86.703097999999997	2624.0055550000002	6183.2559389999997	11650.162974999999	12877.025227	13860.191210000001	14695.567876999999	15406.214986999999	16010.997656	16524.592344000001	16955.382351	17134.617118999999	stress 4	0	1	2.0074999999999998	3.0150000000000001	4.0075000000000003	5.03	6.0025000000000004	7.0049999999999999	8.0075000000000003	9.01	10.032500000000001	11.0175	12.022500000000001	13.0275	14.03	15.012499999999999	16.014999	17.02	18.024999999999999	18.389999	167.180184	4649.0346810000001	12230.839619	17683.848311000002	17494.132922000001	17509.854450999999	17942.741779	17981.523066999998	17953.222398999998	18094.723343000001	



STRESS AND TRUES STRESS VERSE STRAIN GRAPH
σ	0	-3.9056457456496165	-3.2347491740244898	-2.8284510796124351	-2.5316516626113774	-2.3184584421503351	-2.1378049424570778	-1.9802020837356213	-1.8465815685229194	-1.7287292207888791	-1.6243117612573073	-1.5284114368504316	-1.4429897047964357	-1.3673798847905165	0	399.41784446868394	2376.0552303389691	7142.6615458599863	15626.197895513247	26746.442166194553	40118.993320542068	49029.599896754822	56807.704025391016	64562.593318556297	72213.275112276722	79886.932307127849	87237.410793163057	93067.420146063916	ENGINEERING stress (s)	2386.7818140243903	19843.937896341464	60351.802850609747	120848.36187499999	196487.83492378047	271743.85240853654	340241.21213414631	355180.559679878	360053.81964939018	363712.75193597557	366476.96060975606	368346.37269817072	369305.03902439022	365294.56777439022	STRAIN VERSE ENGINEERING STRESS
e1	2386.7818140243903	19843.937896341464	60351.802850609747	120848.36187499999	196487.83492378047	271743.85240853654	340241.21213414631	355180.559679878	360053.81964939018	363712.75193597557	366476.96060975606	368346.37269817072	369305.03902439022	365294.56777439022	0	1.0063976377952756E-2	1.968503937007874E-2	2.9552165354330709E-2	3.9763779527559058E-2	4.9212598425196853E-2	5.895669291338583E-2	6.9020669291338585E-2	7.8887795275590561E-2	8.8754921259842523E-2	9.8523622047244103E-2	0.10843996062992127	0.11811023622047245	0.12738681102362207	e2	2386.7818140243903	19843.937896341464	60351.802850609747	120848.36187499999	196487.83492378047	271743.85240853654	340241.21213414631	355180.559679878	360053.81964939018	363712.75193597557	366476.96060975606	368346.37269817072	369305.03902439022	365294.56777439022	-1	-0.97987204724409449	-0.96062992125984248	-0.94089566929133861	-0.9204724409448819	-0.90157480314960625	-0.88208661417322831	-0.8619586614173228	-0.84222440944881882	-0.82249015748031495	-0.80295275590551185	-0.78312007874015754	-0.76377952755905509	-0.74522637795275581	strain
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		Test Method		ME250L Tensile

		Sample I. D.		2017 Fall Monday night quast

		Specimen Number		2



		EXTENSION (mm)		stress 2		LOGICAL 3 (mm)



		0		85.80169		0

		1		4387.248119		0.084748

		2.0075		8324.902167		0.153423

		3.015		11440.532612		0.360178

		4.0075		13032.151576		0.764191

		5.03		14125.37305		1.23761

		6.0025		14974.376319		1.690573

		7.005		15717.515148		2.164722

		8.0075		16352.695806		2.647639

		9.01		16896.686089		3.138591

		10.0325		17368.354704		3.650001

		11.0175		17754.073854		4.156296

		12.0225		18085.290186		4.681586

		13.0275		18362.002505		5.220026

		14.03		18586.306933		5.770887

		15.0125		18767.636628		6.327593

		16.014999		18910.185036		6.941284

		17.02		19013.952155		7.625842

		18.025		18947.91886		8.417065

		18.389999		18631.376593		8.77359
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Test MethodME250L Tensile

Sample I. D.2017 Fall Monday night quast

Specimen Number 3

EXTENSION (mm)stress 3 LOGICAL 3 (mm)

0 86.7031 0.001461

1.0025 2624.006 0.043835

2.005 6183.256 0.099359

4.005 11650.16 0.580084

5.0075 12877.03 1.02428

6 13860.19 1.468475

7.005 14695.57 1.922899

8.0075 15406.21 2.390473

9.01 16011 2.863891

10.0125 16524.59 3.351922

11.0175 16955.38 3.845797

11.4925 17134.62 4.091273


Microsoft_Excel_Worksheet2.xlsx
Sheet1

		Test Method		ME250L Tensile

		Sample I. D.		2017 Fall Monday night quast

		Specimen Number		3



		EXTENSION (mm)		stress 3		LOGICAL 3 (mm)



		0		86.703098		0.001461

		1.0025		2624.005555		0.043835

		2.005		6183.255939		0.099359

		4.005		11650.162975		0.580084

		5.0075		12877.025227		1.02428

		6		13860.19121		1.468475

		7.005		14695.567877		1.922899

		8.0075		15406.214987		2.390473

		9.01		16010.997656		2.863891

		10.0125		16524.592344		3.351922

		11.0175		16955.382351		3.845797

		11.4925		17134.617119		4.091273
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Test MethodME250L Tensile

Sample I. D.2017 Fall Monday night quast

Specimen Number 4

EXTENSION (mm)stress 4 LOGICAL 3 (mm)

0 167.1802 0

1 4649.035 0.07525

2.005 12230.84 0.218445

3.0025 17683.85 0.355064

4.0175 17494.13 0.794876

5.01 17509.85 1.768015

6.015 17942.74 1.881255

7.0175 17981.52 2.746267

8.0125 17953.22 3.668265

8.7925 18094.72 3.772739
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		Test Method		ME250L Tensile

		Sample I. D.		2017 Fall Monday night quast

		Specimen Number		4



		EXTENSION (mm)		stress 4		LOGICAL 3 (mm)



		0		167.180184		0

		1		4649.034681		0.07525

		2.005		12230.839619		0.218445

		3.0025		17683.848311		0.355064

		4.0175		17494.132922		0.794876

		5.01		17509.854451		1.768015

		6.015		17942.741779		1.881255

		7.0175		17981.523067		2.746267

		8.0125		17953.222399		3.668265

		8.7925		18094.723343		3.772739
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Test MethodME250L Tensile

Sample I. D.2018 Winter Quast Data

Specimen Number 1

Ao (in^2) 42.3225

Lo (mm) 101.6

L20(mm) 50.8

EXTENSION (mm)  ∆ L P(N) Extensometer (mm) (L2)Time (min.) (t)ENG' stress (s)e1  e2 σ  TRUE STRESSε 1 ε 2

0 156.5729 0 0 3.699519 0 -1 0 0 #NUM!

1.0225 1301.762 0.001461 0.05207 30.75817 0.010064 -0.99997 0.000885 0.010014 -10.4565

2 3959.078 0.046757 0.10033 93.54548 0.019685 -0.99908 0.086101 0.019494 -6.99069

3.0025 7927.653 0.111049 0.14859 187.3153 0.029552 -0.99781 0.409472 0.029124 -6.12568

4.04 12889.6 0.198719 0.19939 304.5568 0.039764 -0.99609 1.191362 0.038994 -5.54376

5 17826.4 0.295156 0.24638 421.2038 0.029552 -0.99419 2.44726 0.029124 -5.14815

5.99 22319.82 0.467574 0.29464 527.3749 0.058957 -0.9908 4.854071 0.057284 -4.68809

7.0125 23299.84 1.014051 0.34417 550.531 0.069021 -0.98004 10.9895 0.066743 -3.91394

8.015 23619.53 1.669386 0.39243 558.0845 0.078888 -0.96714 18.33973 0.075931 -3.41544

9.0175 23859.56 2.3123 0.44196 563.7559 0.088755 -0.95448 25.66088 0.085035 -3.08965

10.01 24040.89 2.952292 0.49022 568.0404 0.098524 -0.94188 33.01223 0.093967 -2.84531

11.0175 24163.52 3.614932 0.53848 570.938 0.10844 -0.92884 40.62799 0.102954 -2.64282

12 24226.41 4.265883 0.58547 572.424 0.11811 -0.91603 48.06877 0.11164 -2.47725

12.9425 23963.32 4.89857 0.63119 566.2077 0.127387 -0.90357 54.59858 0.119902 -2.33895
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		Test Method		ME250L Tensile

		Sample I. D.		2018 Winter Quast Data

		Specimen Number		1

		Ao (in^2)		42.322496

		Lo (mm)		101.6

		L20(mm)		50.8

		EXTENSION (mm)  ∆ L 		P(N)		Extensometer (mm) (L2)		Time (min.) (t)		ENG' stress (s)		e1		 e2		σ  TRUE STRESS		ε 1		ε 2



		0		156.572887		0		0		3.6995192108		0		-1		0		0		ERROR:#NUM!

		1.0225		1301.762326		0.001461		0.05207		30.7581652557		0.0100639764		-0.9999712402		0.0008846		0.0100136718		-10.4565305008

		2		3959.078267		0.046757		0.10033		93.5454815094		0.0196850394		-0.9990795866		0.0861005134		0.0194937947		-6.9906876564

		3.0025		7927.652539		0.111049		0.14859		187.3153355369		0.0295521654		-0.9978139961		0.4094720609		0.0291239168		-6.1256800882

		4.04		12889.601971		0.198719		0.19939		304.5567532454		0.0397637795		-0.9960882087		1.1913624695		0.0389935523		-5.543759867

		5		17826.396718		0.295156		0.24638		421.2038136409		0.0295521654		-0.9941898425		2.4472604886		0.0291239168		-5.1481476034

		5.99		22319.823516		0.467574		0.29464		527.3749335578		0.0589566929		-0.9907957874		4.8540710075		0.0572841715		-4.6880940086

		7.0125		23299.844715		1.014051		0.34417		550.5309685657		0.0690206693		-0.9800383661		10.9894976221		0.066742967		-3.9139431548

		8.015		23619.530569		1.669386		0.39243		558.0845366256		0.0788877953		-0.9671380709		18.3397344933		0.0759306913		-3.4154404604

		9.0175		23859.556527		2.3123		0.44196		563.7558930125		0.0887549213		-0.9544822835		25.6608809333		0.0850347693		-3.0896536544

		10.01		24040.888616		2.952292		0.49022		568.040425026		0.098523622		-0.9418840157		33.0122283953		0.0939671165		-2.8453145367

		11.0175		24163.522049		3.614932		0.53848		570.9380195582		0.1084399606		-0.9288399213		40.6279944275		0.1029535859		-2.6428233097

		12		24226.41056		4.265883		0.58547		572.4239553357		0.1181102362		-0.9160259252		48.0687720445		0.1116399711		-2.4772471611

		12.9425		23963.323646		4.89857		0.63119		566.2077124657		0.127386811		-0.9035714567		54.5985849223		0.119902398		-2.3389530288







		Test Method		ME250L Tensile

		Sample I. D.		2017 Fall Monday night quast

		Specimen Number		2



		EXTENSION (mm)		LOAD (N)		LOGICAL 3 (mm)				ENG' stress (s)		e1		 e2		σ  TRUE STRESS		ε 1		ε 2



		0		85.80169		0				2.0273305714		0		-1		0		0		ERROR:#NUM!

		1		4387.248119		0.084748				103.6623198925		0.0098425197		-0.9983317323		0.1729365017		0.0097943976		-6.3959694864

		2.0075		8324.902167		0.153423				196.7015878978		0.0197588583		-0.9969798622		0.5940659		0.0195661859		-5.8024528211

		3.015		11440.532612		0.360178				270.3180032671		0.0296751969		-0.9929098819		1.9165865705		0.0292434096		-4.9490532799

		4.0075		13032.151576		0.764191				332.8393430057		0.0394438976		-0.9849568701		5.0069454797		0.0386858563		-4.1968338756

		4.99		14086.591763		1.217154				332.8393430057		0.0491141732		-0.9760402756		7.974738931		0.0479461636		-3.7313810079

		6.0025		14974.376319		1.690573				353.8160017547		0.0590797244		-0.9667210039		11.7746413294		0.0574003465		-3.4028288299

		7.005		15717.515148		2.164722				371.3749573749		0.0689468504		-0.9573873622		15.8252665449		0.0666739118		-3.1556044078

		8.0075		16352.695806		2.647639				386.3830669628		0.0788139764		-0.947881122		20.13785191		0.0758622677		-2.9542280551

		9.01		16896.686089		3.138591				399.2365216125		0.0886811024		-0.9382167126		24.666144756		0.0849669658		-2.7841223815

		9.9925		17351.584515		3.630275				409.984905309		0.098351378		-0.9285378937		29.2983848843		0.0938103082		-2.6385879516

		11.0175		17754.073854		4.156296				419.4949620646		0.1084399606		-0.9181831496		34.3217565522		0.1029535859		-2.5032720616

		12.0225		18085.290186		4.681586				427.320973366		0.1183316929		-0.9078427953		39.3807064255		0.1118380149		-2.3842594132

		13.0275		18362.002505		5.220026				433.8591586139		0.1282234252		-0.8972435827		44.5818127619		0.1206442054		-2.2753939719

		14.03		18586.306933		5.770887				439.1590451801		0.1380905512		-0.8863998622		49.8885280465		0.129351903		-2.1750705597

		15.0125		18767.636628		6.327593				443.4435206279		0.1477608268		-0.8754410827		55.2348448232		0.1378129371		-2.0829764435

		16.014999		18910.185036		6.941284				446.811668102		0.1576279429		-0.8633605512		61.0521000553		0.1463730347		-1.9904095828

		17.02		19013.952155		7.625842				449.2634875552		0.167519685		-0.849885		67.4411884343		0.1548815713		-1.896353612

		18.025		18947.91886		8.417065				447.7032465193		0.1774114173		-0.8343097441		74.1800654855		0.1633183146		-1.7976351619

		18.389999		18631.376593		8.77359				440.223955435		0.1810039272		-0.8272915354		76.0304034088		0.1663648625		-1.7561502819





		Test Method		ME250L Tensile

		Sample I. D.		2017 Fall Monday night quast

		Specimen Number		3



		EXTENSION (mm)		LOAD (N)		LOGICAL 3 (mm)				ENG' stress (s)		e1		 e2		σ  TRUE STRESS		ε 1		ε 2



		0		86.703098		0.001461				2.0486291262		0		-0.9999712402		0.0000589183		0		-10.4565305008

		1.0025		2624.005555		0.043835				62.0002552543		0.009867126		-0.9991371063		0.0534996297		0.0098187638		-7.0552190485

		2.005		6183.255939		0.099359				146.0985651461		0.019734252		-0.9980441142		0.2857521129		0.0195420561		-6.2369120798

		3.015		9700.601198		0.201641				229.2067367199		0.0296751969		-0.996030689		0.9097928268		0.0292434096		-5.529162745

		4.005		11650.162975		0.580084				275.2711696163		0.0394192913		-0.9885810236		3.1433149834		0.0386621835		-4.4724787129

		5.0075		12877.025227		1.02428				304.2595887303		0.0492864173		-0.9798370079		6.1347836918		0.0481103306		-3.9039064278

		6		13860.19121		1.468475				327.4899289966		0.0590551181		-0.9710930118		9.4667475095		0.0573771126		-3.5436719072

		7.005		14695.567877		1.922899				347.2282891113		0.0689468504		-0.9621476575		13.143404132		0.0666739118		-3.2740624115

		8.0075		15406.214987		2.390473				364.0195272746		0.0788139764		-0.9529434449		17.1295049493		0.0758622677		-3.0564051003

		9.01		16010.997656		2.863891				378.309390259		0.0886811024		-0.9436241929		21.3274972043		0.0849669658		-2.8757151649

		10.0125		16524.592344		3.351922				390.444654871		0.0985482283		-0.9340172835		25.7625989851		0.0939895157		-2.7183624419

		11.0175		16955.382351		3.845797				404.8583788395		0.1084399606		-0.9242953346		30.6496680859		0.1029535859		-2.5809154909

		11.4925		17134.617119		4.091273				404.8583788395		0.1131151575		-0.9194631299		32.6060266569		0.1071625328		-2.519040186



		Test Method		ME250L Tensile

		Sample I. D.		2017 Fall Monday night quast

		Specimen Number		4



		EXTENSION (mm)		LOAD (N)		LOGICAL 3 (mm)				ENG' stress (s)		e1		 e2		σ  TRUE STRESS		ε 1		ε 2



		0		167.180184		0				3.950149443		0		-1		0		0		ERROR:#NUM!

		1		4649.034681		0.07525				109.8478379205		0.0098425197		-0.9985187008		0.1627175158		0.0097943976		-6.5148357299

		2.005		12230.839619		0.218445				288.991453127		0.019734252		-0.9956999016		1.2426916925		0.0195420561		-5.449117367

		3.0025		17683.848311		0.355064				417.8356661904		0.0295521654		-0.9930105512		2.9204410035		0.0291239168		-4.9633535786

		4.0175		17494.132922		0.794876				413.3530527595		0.0395423228		-0.9843528346		6.4678035662		0.0387805421		-4.1574655059

		5.01		17509.854451		1.768015				413.7245225565		0.0493110236		-0.9651965551		14.3990386171		0.0481337808		-3.3580389062

		6.015		17942.741779		1.881255				423.9528259156		0.0592027559		-0.9629674213		15.7000664078		0.0575165081		-3.2959572473

		7.0175		17981.523067		2.746267				424.8691539128		0.0690698819		-0.945939626		22.9685853683		0.0667890012		-2.9176538196

		8.0125		17953.222399		3.668265				424.2004630114		0.078863189		-0.9277900591		30.6314903828		0.075907884		-2.6281775563

		8.7925		18094.723343		3.772739				427.5438609056		0.0865403543		-0.9257334843		31.7521928789		0.0829986616		-2.6000950917






image2.emf
Test MethodME250L Tensile

Sample I. D.2017 Fall Monday night quast

Specimen Number 2

EXTENSION (mm)stress 2 LOGICAL 3 (mm)

0 85.80169 0

1 4387.248 0.084748

2.0075 8324.902 0.153423

3.015 11440.53 0.360178

4.0075 13032.15 0.764191

5.03 14125.37 1.23761

6.0025 14974.38 1.690573

7.005 15717.52 2.164722

8.0075 16352.7 2.647639

9.01 16896.69 3.138591

10.0325 17368.35 3.650001

11.0175 17754.07 4.156296

12.0225 18085.29 4.681586

13.0275 18362 5.220026

14.03 18586.31 5.770887

15.0125 18767.64 6.327593

16.015 18910.19 6.941284

17.02 19013.95 7.625842

18.025 18947.92 8.417065

18.39 18631.38 8.77359


